## Slide 1: Advanced Materials Issues for Supercritical CO2 Cycles FEAA123 (2016 – 2018)
Bruce Pint
Corrosion Science & Technology Group
Materials Science and Technology Division
Oak Ridge National Laboratory
Oak Ridge, TN 37831-6156 USA
Presentation for 2019 Crosscutting Research Project Review Meeting
April 9, 2019

## Slide 2: Acknowledgments
J. Keiser, M. Howell, M. Stephens — oxidation experiments
T. Lowe — SEM, image analysis
T. Jordan — metallography
K. Unocic — TEM
Special thanks for alloys:
  Haynes International
  Special Metals
  ATI
  Sandvik
  Capstone Turbine

## Slide 3: Project is studying materials issues relevant to direct-fired supercritical CO2 cycles
Goals and Objectives
  Address materials issues for scaling up direct-fired sCO2 Brayton cycles to higher temperatures for increased efficiency and larger size for commercial power generation
Milestones
  FY16
    Data analysis on effect of temperature on reaction rates (6/16, complete)
    1 and 25 bar testing at three different impurity levels (8/17, complete)
    Complete construction of test rig capable of studying impurity effects in sCO2 (9/17, complete)
  FY17
    Complete analysis of reaction products as a function of temperature, pressure, etc. (12/17, complete)
    Complete 500h exposures at three different impurity levels in 300 bar sCO2 (2/18, complete)
    Complete 2,500 h of cumulative exposure in sCO2 with a high H2O content (6/18, complete)
  FY18
    Compare 2,500 h sCO2 reaction products formed with and without O2 and H2O (9/18, complete)
    Complete 5,000h with a high H2O content to quantify reaction rate effects (12/18, complete)
    Complete a time series of 25°C tensile properties at 750°C/300 bar w/o impurities (12/18, complete)

## Slide 4: Supercritical CO2 Allam cycle: first clean fossil energy?
NetPower 25MWe demo plant (Texas)
Exelon, Toshiba, CB&I, 8Rivers Capital: $140m
Material challenges:
Combustor: 1150°C (!?!)
Turbine exit: 750°C/300 bar
Combustion impurities: O2, H2O, SO2
Moving forward with limited compatibility data!
As audacious as Eddystone in 1960
May 2018: announced first firing

## Slide 5: Fossil/Solar focus on >700°C for high efficiency sCO2
>700°C: favors precipitation-strengthened Ni-based alloys
Low critical point (31°C/7.4 MPa)
High, liquid-like density
Flexible, small turbomachinery
Feher, 1965
50% sCO2 eff @ >720°C
sCO2 applications
740/282 above 700°C

## Slide 6: Indirect- vs. direct-fired sCO2 systems (i.e. closed vs. open)
Closed cycle:
“pure” CO2 100-300 bar
Open cycle:
sCO2 + impurities (O2,H2O…)
DOE SunShot funding
DOE Fossil Energy funding

## Slide 7: Two sCO2 projects completing at ORNL
DOE Fossil Energy (2015-2018)
750°C/300 bar: 500-h cycles
Focus on impurity effects for direct-fire
  Baseline research grade (RG) CO2
  New autoclave with controlled O2+H2O
Alloys
  310HCbN (HR3C, Fe-base SS)
  617
  230
  247 (Al2O3-forming superalloy)
  282 (Heat #1)
  740
DOE SunShot (CSP) (2015-2018)
750°C/300 bar: 500-h cycles
  Including 750°C/1 bar, 10-h cycles
Focus on industrial grade (IG) CO2
  Indirect fired (closed loop)
Alloys
  Alloy 25 (Fe-base SS Sanicro 25)
  625
  740
  282 (Heat #2)
 | Air | RG CO2 | IG CO2 | FE: CO2+O2/H2O
1 bar | 5,000 h | 5,000 h | 5,000 h | –––
300 bar | ––– | 5,000 h | 5,000 h | 5,000 h
Cooperative test matrix:
FE
FE
FE/CSP
CSP

## Slide 8: Thermodynamics: Oxygen levels similar in steam/CO2 Concern about high C activity at m-o interface
Factsage calculations
High carbon activity at Ptotal = 1 bar
What is Pinterface?
2CO(g) = C(s) + CO2(g) CO2(g) = 0.5O2 + CO(g)

## Slide 9: Range of alloys have been evaluated
 | Ni | Cr | Fe | Co | Refractories | Ti | Al | S | Other
Grade 91 | 0.1 | 8.3 | 90 | 0.01 | 0.9Mo,0.1Nb | <0.01 | <0.01 | 10 | 0.03Cu,0.3Mn,0.1Si,0.3V
304H | 8.4 | 18 | 70 | 0.1 | 0.3Mo,0.01Nb | <0.01 | <0.01 | 29 | 0.4Cu,1.6Mn,0.3Si,0.07N
25 | 25 | 22 | 43 | 1.5 | 3.5W,.5Nb,.2Mo | 0.02 | 0.03 | 8 | 3.0Cu, 0.5Mn, 0.2Si, 0.2N
310HCbN | 20 | 25 | 51 | 0.3 | 0.1Mo,0.4Nb | 0.01 | <0.01 | <10 | 0.1Cu,1.2Mn,0.3Si,0.3N
230 | 61 | 23 | 2 | 0.1 | 1Mo, 12W | 0.01 | 0.3 | 9 | 0.02La
625 | 61 | 22 | 4 | 0.1 | 9Mo, 4Nb | 0.2 | 0.1 | <10 | 0.2Si,0.1Mn,0.02C
617 | 54 | 22 | 1 | 13 | 9Mo, 1Nb | 0.3 | 1.1 | <3 | 
740 | 48 | 23 | 2 | 20 | 0.3Mo, 2Nb | 2.0 | 0.8 | <10 | 0.5Si,0.3Mn,0.03C
282 | 58 | 19 | 0.2 | 10 | 8Mo | 2.2 | 1.5 | <1 | 0.1Si,0.1Mn,0.06C
247 | 60 | 8 | 0.03 | 10 | 10W,3Ta,1Mo | 1.1 | 5.3 | <1 | 1.3Hf,0.14C
Compositions measured using ICP-OES and combustion analyses

## Slide 10: CO2 compatibility evaluated several ways at 700°-800°C
Autoclave: 300 bar sCO2
500-h cycles
Previously:
”Keiser” rig:
500-h cycles, 1-43 bar CO2
Tube furnace: 1 bar CO2
500-h cycles
Study impurities at 1-43 bar
Correct temperature and pressure
Same cycle frequency as autoclave
Baseline of research grade (RG) CO2: ≤ 5 ppm H2O and ≤ 5 ppm O2
industrial grade (IG) CO2: 18±16 ppm H2O and ≤ 32 ppm O2
Baseline:
Box furnace:
Lab. Air
500-h cycles
4-5 cm2 alloy coupons

## Slide 11: Impurities (2015): 1atm, many alloys (1 of each)
700°C
800°C

## Slide 12: Impurities (2017): fewer alloys (3 of each), 1 and 25 bar
304H
230
282
247
(Al2O3-fomer)
Two alloy 230 reaction tubes:
Pressure: 1 and 25 bar
Gas: RG CO2
CO2+10%H2O
CO2+10%H2O+0.1%SO2
Pint, Brese, Keiser, NACE Corrosion 2018 C2018-11199

## Slide 13: CSP: completed 10,000 h exposures for lifetime model
500-h cycles: three different environments
Quantification of scale thickness in three environments:
Extrapolation sCO2 to 100,000 h
Pint, Keiser, NACE Corrosion 2019 C2019-12750

## Slide 14: 2016-2017: baseline performance in RG and IG sCO2
Research grade (RG) CO2: ≤ 5 ppm H2O and ≤ 5 ppm O2
Industrial grade (IG) CO2: 18±16 ppm H2O and ≤ 32 ppm O2
Similar mass gain in RG & IG sCO2
Sanicro 25
Fe-22Cr-25Ni

## Slide 15: 2018: finally completed multi-pump 300 bar autoclave Clearly see an effect of impurities
Industrial grade (IG) CO2: 18±16 ppm H2O and ≤ 32 ppm O2
Goal: 1%O2+0.25%H2O
(industry suggestion)
Not easy to control at 300 bar
Lower mass gain in IG sCO2
Sanicro 25
Fe-22Cr-25Ni

## Slide 16: Summary: impurities caused a higher mass gain
RG CO2 + 1%O2 + 0.25% H2O

## Slide 17: Metallography consistent with mass change

## Slide 18: Fe-based alloys: strongest effect

## Slide 19: SEM/EDS: Fe/Ni-rich oxide forming with impurities
1000 h at 750°C, 300 bar sCO2+1%O2+0.25%H2O

## Slide 20: GDOES: very different oxide forming on 25: (Fe-22Cr-25Ni)
RG sCO2
sCO2+1%O2+0.25%H2O
1000 h at 750°C, 300 bar
Glow discharge optical emission spectroscopy

## Slide 21: 625 (NiCr) 1000h STEM: unusually thick Cr-rich oxide layer
Scanning transmission electron microscopy
Scale thickness 3.70±44µm
1000 h at 750°C, 300 bar sCO2+1%O2+0.25%H2O
STEM annular dark field image

## Slide 22: Measuring 25°C tensile properties suggests future strategy: Post 750°C exposure shows drop in ductility Method to quantify degradation of steels at 450°-650°C (?)
Yield strength
Elongation:
25mm
dogbone
304H: large drop in sCO2
310: also degrading, w/o impurities
Pint, et al., Materials and Corrosion, 2019, on-line

## Slide 23: Project is concluding having achieved its goals
Developed new experimental equipment for studying impurity effects on structural materials at up to 750°C/300 bar
Results indicate that there is a negative effect of impurities, more so for Fe-based alloys than Ni-based alloys
Room temperature tensile data suggests a simple route to quantify sCO2 impact on mechanical properties of steels exposed at lower temperatures
Industrial collaborations
All major US alloy manufacturers
Conference calls conducted with HX, sCO2 community (CSP project)
Feedback from 8 Rivers/NetPower on impurity levels of interest
Public presentations (TMS, MS&T, EFC workshop, NACE, EU sCO2)

## Slide 24: Backups

## Slide 25: FE project studying model Ni-22Cr alloy specimens
Scale
W-protective layer
BF-STEM
750°C, Air, 1000h
2µmz
Scale
BF-STEM
750°C, 300 bar sCO2, 1000h
Alloy
Line 7
Line 1
Line 6
EDS Line 1
EDS Line 2
Air only: Metallic Ni particles in scale near substrate interface
C on oxide grain boundaries
Line 2

## Slide 26: 500h at 800°C: SO2 suppressed internal oxidation at 1 bar
Similar results for SO2 reported by Young (UNSW) and Quadakkers (Jülich)
Cr2O3-former
Al2O3-former
10%H2O+1000 ppm SO2

## Slide 27: 500h at 800°C: at 25 bar, 0.1%SO2 resulted in more attack
Haynes 282: Ni-20Cr-11Co-9Mo-1.6Al-2.2Ti
MarM247 superalloy: Ni-9Cr-10Co-1Mo-6Al-10W-3Ta-1.4Hf
10%H2O+1000 ppm SO2
10%H2O+1000 ppm SO2
NACE 2018 paper

## Slide 28: Success warrants continued work to answer more q’s
Complete characterization and publications in early 2019
  Mount 5,000 h specimens, etching, TEM, EPMA, etc.
New FWP to focus on:
  Mechanistic understanding of O2/H2O effects with 18O/H218O tracers
    Separate O2 and H2O effects
  Focus on steels at lower temperatures: technology enabler
    #1 question from industry is ”where can I use T91?”: cheaper and strong vs. fear
    Provide input to alloy designers on effect of Cr/Ni in Fe-Cr-Ni alloys
    Use 25mm tensile bars to assess sCO2 effect on strength & ductility
  Surface modifications to improve steel performance (as warranted)
    Shot peening
    Coatings
  Creep assessment of thin-walled material at 750°C (282/740/etc.)
  Model lifetime as a function of temperature/HX dimensions/heat transfer