## Slide 1: Materials Research For Supercritical CO2 Power Cycles High-temperature corrosion of Ni-based alloys and steels
UTSR, Nov. 5-7, 2019, Orlando, FL
Ömer Doğan1, Richard Oleksak1,2, Joe Tylczak1, Gordon Holcomb1
1National Energy Technology Laboratory, 1450 Queen Ave SW, Albany, OR 97321, USA
2Leidos Research Support Team

## Slide 2: Acknowledgements
This work was performed in support of the U.S. Department of Energy’s Fossil Energy Crosscutting Technology Research Program. The Research was executed through the NETL Research and Innovation Center’s Advanced Alloy Development Field Work Proposal. Research performed by Leidos Research Support Team staff was conducted under the RSS contract 89243318CFE000003.
DISCLAIMER
This work was funded by the Department of Energy, National Energy Technology Laboratory, an agency of the United States Government, through a support contract with Leidos Research Support Team (LRST). Neither the United States Government nor any agency thereof, nor any of their employees, nor LRST, nor any of their employees, makes any warranty, expressed or implied, or assumes any legal liability or responsibility for the accuracy, completeness, or usefulness of any information, apparatus, product, or process disclosed, or represents that its use would not infringe privately owned rights. Reference herein to any specific commercial product, process, or service by trade name, trademark, manufacturer, or otherwise, does not necessarily constitute or imply its endorsement, recommendation, or favoring by the United States Government or any agency thereof. The views and opinions of authors expressed herein do not necessarily state or reflect those of the United States Government or any agency thereof.

## Slide 3: Direct sCO2 Power Cycles
Cycle Type | Component | Inlet |  | Outlet |  | Fluid components
 |  | T (°C) | P (MPa) | T (°C) | P (MPa) | 
Indirect | Heater | 450-535 | 1-10 | 650-750 | 1-10 | High purity CO2
 | Turbine | 650-750 | 20-30 | 550-650 | 8-10 | 
 | HX | 550-650 | 8-10 | 100-200 | 8-10 | 
Direct | Combustor | 750 | 20-30 | 1150 | 20-30 | CO2 containing H2O, O2, and other impurities based on fuel (e.g., SO2)
 | Turbine | 1150 | 20-30 | 800 | 3-8 | 
 | HX | 800 | 3-8 | 100 | 3-8 | 
This project aims to reduce technical risks to commercialization of the direct supercritical CO2 power cycle technology by
  generating alloy performance data
  demonstrating the long-term durability of commercial materials in direct sCO2 power cycle environment

## Slide 4: High-temperature oxidation exposures
Gas 1 (vol%): CO2, 4% H2O, 1% O2
Gas 2 (vol%): CO2, 4% H2O, 1% O2, 0.1% SO2
Pressure: 1 bar, 200 bar
Temperature: 550-750 °C
Duration: Up to 2500 h (500 h increments)
exposure samples
H2O inlet
CO2/O2/SO2 inlet
Pt-Rh catalyst mesh
NETL sCO2 Autoclave
Gas: CO2, H2O, and O2
Max. pressure: 275 bar
Flow rate: 2 ml/min
Max. Temperature: 800°C
Argon purging

## Slide 5: Steels
Alloy | Fe | Ni | Cr | Co | Mo | Mn | W | Nb | Si | Ti | Al | C
Ferritic/Martensitic |  |  |  |  |  |  |  |  |  |  |  | 
GR-22 | 95.5 | 0.15 | 2.29 | 0.02 | 0.99 | 0.45 | <0.010 | 0.005 | 0.27 | 0.001 | 0.03 | 0.1
GR-91 | 88.78 | 0.19 | 8.72 | 0.02 | 0.95 | 0.44 | <0.010 | 0.075 | 0.29 | 0.003 | 0.07 | 0.11
MARBN3 | 83.16 | 0.17 | 9.6 | 2.95 | 0.1 | 0.5 | 2.89 | 0.057 | 0.2 | <0.001 | 0.011 | 1.5
CPJ7 | 85.5 | 0.27 | 9.88 | 1.46 | 1.36 | 0.31 | 0.37 | 0.056 | 0.31 | 0.003 | 0.02 | 0.15
MARBN4 | 82.68 | 0.17 | 10.1 | 2.94 | 0.1 | 0.5 | 2.89 | 0.056 | 0.19 | <0.001 | 0.011 | 1.53
SAVE 12 | 82.8 | -- | 10.5 | 2.92 | -- | 0.51 | 2.87 | 0.07 | 0.23 | -- | -- | 0.11
409 | 86.82 | 0.29 | 11.52 | 0.03 | 0.02 | 0.44 | <0.010 | 0.01 | 0.36 | 0.165 | 0.1 | 0.08
420 | 85.96 | 0.42 | 12.37 | 0.02 | 0.09 | 0.49 | 0.02 | 0.005 | 0.25 | 0.01 | 0.05 | 0.22
416 | 85.45 | 0.28 | 12.45 | 0.02 | 0.2 | 1.08 | 0.01 | 0.014 | 0.22 | 0.009 | 0.01 | 0.13
E-Brite | 71.6 | 0.21 | 26.5 | 0.02 | 1 | 0.04 | <0.010 | 0.12 | 0.25 | <0.001 | 0.1 | 0.01
Austenitic |  |  |  |  |  |  |  |  |  |  |  | 
347H | 70.1 | 9.01 | 17.3 | 0.14 | 0.37 | 1.86 | -- | 0.52 | 0.31 | 0 | 0.007 | 0.05
304H* | 70.6 | 8.27 | 18.74 | 0.22 | 0.12 | 1.08 | 0.01 | 0.01 | 0.44 | 0.003 | 0.01 | 0.07
800 | 44.2 | 32.74 | 19.87 | 0.07 | 0.2 | 0.91 | <0.010 | 0.05 | 0.46 | 0.46 | 0.37 | <0.1
310S | 53.5 | 19.1 | 25 | 0.17 | 0.09 | 1.39 | -- | 0.01 | 0.39 | 0 | 0.02 | 0.04
Increasing Cr content

## Slide 6
Critical Cr content
2
9
10
11
10
12
10
12
12
27
17
19
20
25
Cr content (wt%)
CO2 - 4% H2O - 1% O2
CO2 - 4% H2O - 1% O2- 0.1% SO2
2
9
10
11
10
12
10
12
12
27
17
19
20
25
Cr content (wt %)
550°C
600°C
650°C
550°C
600°C
650°C
At least, 12 % Cr is necessary to form a protective scale on steels between 550 and 650°C
No significant effect of SO2 on low Cr (2-9 wt%) steels.
More substantial effect on the austenitic stainless steels.

## Slide 7
Minimal sulfur effect in Gr.91
Qualitative X-ray mapping of Gr-91 exposed at 550 °C and 1 atm to 95% CO2, 4% H2O, 1% O2, 0.1% SO2 for 2250 h
Duplex oxide scale consisting of an outer layer of Fe2O3/Fe3O4 and inner layer of Fe-Cr spinel.
Internal oxidation zone (IOZ) immediately below the oxide scale when no SO2 present. Thinner or no IOZ when SO2 present.
FeS particles near the outer/inner oxide scale interface.
IOZ
550°C

## Slide 8
Sulfur effect in 347H
Qualitative X-ray mapping of 347H exposed at 550 °C and 1 atm to 95% CO2, 4% H2O, 1% O2, 0.1% SO2 for 2250 h
Frequent, large Fe-rich oxide nodules
Small sulfide particles in the alloy substrate
Sulfide particles more prevalent beneath the thick oxide nodules
Thin Cr oxide scale formed on the entire surface initially, then failed where the thick oxide nodules formed. Eventually a new Cr-oxide scale formed.
550°C

## Slide 9
Internal carburization in Gr.91
Extent of internal carburization of Grade 91 was reduced in SO2 at 550°C

## Slide 10: Ni alloys
wt% | Fe | Ni | Cr | Co | Mo | Mn | W | Nb | Si | Ti | Al | C
Ni-based (solution strengthened) |  |  |  |  |  |  |  |  |  |  |  | 
600 | 7.6 | 75.0 | 16.0 | 0.1 | 0.2 | 0.2 | <0.010 | 0.1 | 0.2 | 0.3 | 0.1 | -
617 | 0.4 | 55.1 | 21.9 | 11.5 | 9.6 | 0.04 | <0.010 | 0.03 | 0.02 | 0.5 | 0.9 | -
230 | 0.4 | 59.8 | 22.2 | 0.3 | 1.3 | 0.5 | 14.4 | 0.04 | 0.4 | 0.01 | 0.4 | -
625 | 4.4 | 60 | 22.3 | 0.03 | 8.3 | 0.4 | - | 3.5 | 0.2 | 0.2 | 0.1 | 0.1
Ni-based (precipitation strengthened) |  |  |  |  |  |  |  |  |  |  |  | 
718 | 18.1 | 53.8 | 18.0 | 0.2 | 3.0 | 0.2 | - | 5.3 | 0.1 | 1.0 | 1.6 | 0.1
282 | 0.2 | 58.2 | 19.3 | 12.1 | 8.4 | 0.1 | - | 0.02 | 0.2 | 2.1 | 1.3 | -
263 | 0.4 | 50.7 | 20.3 | 19.7 | 5.8 | 0.4 | - | 0.08 | 0.02 | 2.2 | 0.4 | 0.1
740H | <0.010 | 50.4 | 24.5 | 20.2 | 0.3 | 0.2 | <0.010 | 1.5 | 0.1 | 1.4 | 1.2 | -
Several commercially available Ni-based alloys were tested:
Increasing Cr content

## Slide 11
Mass change (750 °C)
Low mass gains for all Ni alloys—notably higher for Alloy 263.
XRD identified corrosion products as Cr2O3 with minor spinel oxide and TiO2.
Little or no effect of SO2.
No SO2
0.1% SO2

## Slide 12
Alloy 740H (750 °C, 2500 h)
No SO2
0.1% SO2
Chromia scale and internal oxidation of Al.
Sub-surface voiding and recrystallization.*
Similar observations for most Ni alloys.
No effect of SO2, consistent with mass gains.
Cross-sectional SEM
Oleksak et al., Structural evolution of a Ni alloy surface during high-temperature oxidation, Oxid. Met. (2017)
Oleksak et al., The role of metal vacancies during high-temperature oxidation of alloys, npj Mater. Degr. (2018)
*

## Slide 13
Mass change (650 °C)
Low mass gains and no significant effect of SO2, similar to exposures done at 750 °C.
XRD confirmed primary reaction product = chromia.
No SO2
0.1% SO2

## Slide 14
Mass change (600 °C)
1-2 orders of magnitude higher mass gains in the presence of SO2.
Alloy 617 appears to be the most affected.
No SO2
0.1% SO2

## Slide 15
Surface SEM
Alloy 617 (600 °C, 0.1% SO2, 2500 h)
Large nodules are formed in presence of SO2.
EDS confirmed surface rich in Ni, Co, O, S.

## Slide 16
XRD of alloy 617 (600 °C, 2500 h)
Only thin protective Cr2O3 layer formed in the absence of SO2.
Non-protective oxides and sulfates formed in SO2 exposure.
substrate
Cr2O3
NiO
NiSO4·6H2O
Co(CrO4)
No SO2
0.1% SO2

## Slide 17
EPMA mapping reveals
Large outward-growing Ni-oxide nodules
Sulfur at the outermost surface (likely NiSO4)
Cr-rich oxides and sulfides formed internally
Alloy 617 (600 °C, 0.1% SO2, 2500 h)
BSE
Ni
O
S
Cr
Co

## Slide 18
Effect of SO2 (alloy 617, 600 °C, 2500 h)
Extent of corrosion consistent with mass change data: ≈1-2 orders of magnitude higher in presence of SO2 at 600 °C
Ni and/or Co sulfates + Co(CrO4)
Ni-oxide
Failed chromia scale
Cr-rich oxides + sulfides
Protective chromia scale
No SO2
0.1% SO2

## Slide 19: Summary
Several commercially available Ni-based alloys and steels were exposed to high-temperature CO2 containing H2O, O2, with and without SO2 at 1 bar to simulate composition expected in direct-fired sCO2 power cycles.
Steels at 550-650°C:
  There was a critical Cr content between 11 and 12 wt % above which a thin protective oxide scale formed.
  The steels containing less than 11 wt % Cr formed thick duplex Fe-rich oxide scales.
  The addition of SO2 to the environment did not make a significant change in corrosion rates.
  Extent of internal carburization of Grade 91 was reduced in SO2 at 550°C

## Slide 20: Summary
Ni-based alloys:
  At temperatures of 650-750 °C:
  All alloys formed thin chromia scale leading to low corrosion rates.
  No effect of SO2.
  At temperature of 600 °C:
  Thin chromia scales leading to low corrosion rates in absence of SO2.
  Significantly higher corrosion rates (1-2 orders of magnitude) with 0.1% SO2, characterized by growth of non-protective oxides and sulfates.
  Ni-based alloys are suitable in the absence of SO2, however caution is needed when extrapolating corrosion performance to lower temperatures when SO2 is present.