## Slide 1: Improved Performance Thermal Barrier Coatings Using The Solution Precursor Plasma Spray Process
Maurice Gell, Eric Jordan,
Jeffrey Roth, Rishi Kumar
University of Connecticut
+
+
-
UTSR SBIR Phase IIA Presentation
November 4, 2015
Jiwen Wang, Chen Jiang Balky Nair
HiFunda LLC

## Slide 4
Liquid reservoir
Plasma gun
Droplets
Coating
Substrate
Temperature
control unit
Solution Precursor Plasma Spray (SPPS) Process
A
B
Liquid
injector
Solution Precursors
A, B or A+B
Multiple composition

## Slide 5
3 SPPS TBCs Developed
SPPS TBC
Benefits
YSZ
High Durability
YSZ with IPBs
Lower K
High Durability
YAG
Higher Temp.
Lower K
High Durability
Lower Density

## Slide 6
Solution Precursor Plasma Spray:
Unique Microstructural Features
100 μm
1 μm
Through-thickness vertical cracks
Varied nano/micro-scale porosity:
0~40%
Splat diameter < 2 μm
Splat thickness < 1 μm
Splat area is 1/2500 of that in APS TBCs
Layered porosity: inter-pass boundaries.

## Slide 7
SPPS
500 m
Thick SPPS Thermal Barrier Coatings
Substrate
4mm
Surface

## Slide 8
0
0.2
0.4
0.6
0.8
0
0.5
1.0
1.5
2.0
2.5
3.0
Thermal Cycle:
1121°C/1 hour
0
100
200
300
400
500
0
1
2
3
Substrate A
Substrate B
Coating Thickness (mm)
Spallation Life, Cycles
Normalized Crack Spacing
Coating Thickness (mm)
Effect of SPPS TBC Thickness On Durability

## Slide 9
SPPS can Make Thin Dense Layers 10 Micron

## Slide 10
1 m
1 m
Ultra-Fine Splats Formed In The SPPS Process
Splat diameter: < 2 m
Splat thickness: < 1 m
Splat area is 1/2500 of splats in APS TBCs

## Slide 11
In-Plane Fracture Toughness
In Plane Fracture Toughness (MPam1/2)
400 m
400 m
100 m
100 m
APS
TBC
SPPS
TBC

## Slide 12
Engineered SPPS YSZ TBC Architecture
10 m
Vertical cracks for strain tolerance/thermal cycle durability
Planar pores (IPBs) for low thermal conductivity

## Slide 13: SPPS YSZ With IPBS: Thermal Conductivity
50% Reduction Demonstrated
Notes: Enter speaker notes here.

## Slide 14: Properties Of YSZ and YAG
Material Property | YSZ | YAG
Melting Point (oC) | 2680 | 1950
Maximum Operating Temperature (oC) | 1200-1300 | 1800
Thermal Conductivity at 1350 oC (W/mol-K) | 2.0-3.0 (measured) | 2.5 (extrapolated)
Thermal Expansion Coefficient (ppm/K) |  | 
Density (g/cc) | 6.10 | 4.55
Vickers Hardness | 1200 | 1700

## Slide 15
SPPS YAG TBCs: Project Objectives
Develop a Higher Temperature (+200oC), Lower Thermal Conductivity Thermal Barrier Coating Using Yttrium Alumina Garnet (YAG) and the Solution Precursor Plasma Spray Process (SPPS)
Phase IIa Objective Improve Performance/Cost ratio.

## Slide 16
Anticipated Benefits
A New TBC That Can Tolerate Surface Temperatures of 1500oC Can Be Game-Changing For the Gas Turbine Industry Due to Higher Turbine Efficiencies and Lower Fuel Consumption

## Slide 17
Yttria-Alumina Phase Diagram
M. Shojaie-Bahaabad et al,
Ceramics Intl.,Vol 35, 2009

## Slide 18: Performance

## Slide 19: Thermal Spray Optimization Many Variables
Stand off Distance
Precursor Composition
Atomizing Gas Pressure
Scan Speed and Step Height
Injection Method, Stream vs. Atomizing
Feed Rate
Gun Power
Gas Mix
Gun Type

## Slide 20
SD = 1.375” 1.425” 1.5” 1.625”
Increased Spray Distance at Lower Atomizing Pressure

## Slide 21
SPPS YAG TBCs: Standard Microstructure
--Used for Engine-Critical Properties Tests--
SPPS YAG
APS YSZ
Bond Coat
Superalloy
Vickers Hardness: 200-400
Porosity: 15-20%

## Slide 22
SPPS YAG TBCs: Critical Engine Properties
200oC Temperature Advantage
Phase Stability
Sinter Resistance
CMAS Resistance
Improved Durability
Thermal Cycle Resistance
Erosion Resistance
Other Significant Properties
Lower Thermal Conductivity
Reduced Density
Surface Smoothness

## Slide 23
M: YAM
P: YAP
M
P
As-Sprayed SPPS YAG
As-Sprayed SPPS YAG with Excess Al3+ in precursor
Predominantly YAG Phase with Minor Amounts of YAM and YAP
Pure YAG phase
Stoichiometric YAG Deposited By SPPS Process
Intensity

## Slide 24
SPPS YAG TBCs: Phase Stability
SPPS YAG TBCs Are Phase Stable To At Least 1600oC
M: YAM
P: YAP
M
P
M: YAM
P: YAP
M
P
1500ºC 100 hr
As-sprayed SPPS YAG
M
P
1600ºC 100 hr
M: YAM
P: YAP

## Slide 25
APS YSZ
Thermal Conductivity of SPPS YAG TBCs
Measured by Netzsch Instruments Using Laser Flash
1 mm thick sample with Vickers Hardness of 246
SPPS YAG

## Slide 26
Chart: Thermal Conductivity (W/m-K)
| SPPS YAG without IPBs | SPPS YAG with partial IPBs (Netzsch Sample) | SPPS YAG with IPBs
 | 2.05 | 1.65 | 0.99
Porosity ~23%
HV= 324±60
Porosity ~33%
HV= 260 ±33
Porosity ~15%
HV= 249±175
Thermal Conductivity of different YAG samples

## Slide 27
As-sprayed
1500ºC 100h
1600ºC 100h
SPPS YAG TBCs: Sintering Resistance
HV = 324±122
HV = 380±185
HV = 378±139
Sintering Effects Are Small Up to 1600oC

## Slide 28
SPPS TBCs: Sintering & Thermal Conductivity
SPPS YAG TBCs More Sinter Resistant Than SPPS and APS YSZ
Chart: Sintering Temperature ˚C
| 1150 | 1250 | 1350
SPPS YSZ | 21.4461 | 42.2794 | 76.2255
SPPS YAG | 4.419 | 7.9929 | 16.4544
 | 30.1088
SPPS YSZ 50 hrs
SPPS YAG
50 hrs
20 hrs

## Slide 29
G: YAG
1500 ֯C
1400 ֯C
1300 ֯C
1200 ֯C
1100 ֯C
1500 °C
Phase Stability: 50:50 w/o YAG/CMAS Powder
YAG Phase Stable To 1500oC In Presence of CMAS

## Slide 30: Spritz/Atomizer Test Conditions
4-CMAS (M.P. ~1200 oC )
9-CMAS (M.P. ~1180 oC)
Time (min)
Temperature
1180 oC
0
10
20
30
40
50
60
Oxide | SiO2 | CaO | Al2O3 | MgO
Wt.% | 52.3 | 37.1 | 7.1 | 3.5
Mol.% | 51.5 | 39.2 | 4.1 | 5.2
Oxide | CaSO4 | SiO2 | CaO | Al2O3 | MgO | Fe2O3 | K2O | TiO2 | Na2O
Wt.% | 42.00 | 31.57 | 1.54 | 16.50 | 2.66 | 1.54 | 1.54 | 1.33 | 1.32
Mol.% | 26.75 | 45.56 | 2.38 | 14.03 | 5.72 | 0.84 | 1.42 | 1.44 | 1.85
1 wt% CMAS Aqueous Solution
0.1 mL/spray

## Slide 31: Spritz Test: Cyclic Lives
4 Component CMAS
9 Component CMAS

## Slide 32
SPPS YAG TBCs: Thermal Cycle Life vs Hardness
MAX
SPPS Strain-Tolerant Microstructure Overcomes
Higher Thermal Expansion Mismatch Stresses
MIN
AVERAGE

## Slide 33
SPPS YAG TBCs: Erosion Rate vs Hardness
(Tests Performed at Penn State Univ. By Dr. D Wolfe)

## Slide 34
YSZ
YAG
hardness
SPPS YAG TBCs: Erosion Rate vs Hardness
(Tests Performed at Penn State Univ. By Dr. D Wolfe)

## Slide 35
SPPS YAG TBCs: Erosion Rate vs Hardness
-30º Impingement-
(Tests Performed at Penn State Univ. By Dr. D Wolfe)
SPPS YAG Has Superior Erosion Resistance To APS YSZ In Both 30º
90º Impingement Erosion Tests.

## Slide 36: Cost Reduction- Utility Improvements

## Slide 37: Phase IIA Industry Partners
Solar Turbines
Siemens Energy
Pratt & Whitney
Praxair
Progressive Surface
Chromalloy
General Electric Power
Rolls-Royce
Oerlikon-Metco

## Slide 38: Industrial Partners Activities
Olikon Metco spray trials done
Praxair spray trials in progress this week
Solar Engine Parts sprayed and delivered
Progressive Spray trials scheduled
Outside of Phase IIa we are involved in Tech Transfer

## Slide 39: Goals Related to Industrialization Benefits Cost Ratio
Lower Thermal Conductivity(less thickness)
Higher Deposition Efficiency
Higher Deposition Rate
Larger Stand off Distance

## Slide 40
Conductivity reduction via rare earth Doping
SPPS YAG coatings were produced with 1 atm.% doping of a Rare Earth
~24% reduction in thermal conductivity was achieved at RT
Chart: 
| Undoped YAG | Doped
 | 2.08 | 1.58
XRD showing phase stability
Comparison of Thermal conductivity
SEM images of SPPS YAG coatings with 1 atm.% doping

## Slide 41: Improved Deposition Efficiency from 24% to 42%
Chart: 
| Deposition Efficiency (%) | Deposition Rate (um/pass) | Cost per 50um coating ($) | Viscosity (cP)
Acetate Precursor | 42 | 7.725 | 21.4775 | 2.8
Nitrate Precursor(10% Diluted) | 23.6 | 6.23 | 36.1325 | 4.8

## Slide 42
Chart: Temperature (˚C)
Improved Using Acetate Vs. Nitrate Precursor
YAG peaks are visible (in red) with some YAP phase (in blue)
DSC
XRD of heat treated precursor for 5 hours at 1200˚C
Crystallization of YAG
Substantial increase in DE and DR leads to a 40% reduction in production cost of SPPS YAG coatings with Acetate precursor
Lower Viscosity helps in more uniform flow, less clogging and buildup at the nozzle
Stronger exothermic peaks during decomposition aids in melting of YAG particles in plasma

## Slide 43: Diluted Nitrate Precursor Increased DE and Reduced Cost
15% Dilution, SD: 1.375’’
HV: 374 ± 54
30% Dilution, SD: 1.5’’
HV: 229 ± 25
50% Dilution, SD: 1.5’’
HV: 250 ± 25
25% Dilution, SD: 1.375’’
HV: 243 ± 48
Repeatable microstructures and hardness were produced with all the precursors
Chart: Dilution of YAG precursor
| 10 | 15 | 25 | 30 | 50
Deposition Efficiency | 23.6 | 26.1 | 25.6 | 26.75 | 32.3
Deposition Rate | 6.23 | 4.95 | 4.96 | 4.65 | 4.46
Chart: Dilution (%)
| 10 | 15 | 20 | 30 | 50
 | 144.53 | 139.92 | 137.94 | 134.65 | 136.91

## Slide 44
Standoff Distances
Industrial Partner Visits | STTR Phase | Plasma Gun Used | Standoff Distance (inch) | Results/ Comments | Future work
Praxair 11/2014 | 2 | F-4 | 1.5-3.0 | Poor- Fair initial results | F-4, 100HE, Plazjet, HE1100
Progressive 02/2015 | 2 | 100HE | 2.0-2.75 | Fair initial results | 100HE itself
Progressive 05/2015 | 2a | 100HE | 2.0-2.75 | Good, Columnar structure, Vickers Hardness-400 | Spray B/C, APS YSZ and SPPS YAG for Thermal Cycling
Metco 09/2015 | 2a | Sinplex Pro | 2.25-2.75 | Initial testing with YSZ, Good results | Spray YAG
Praxair 11/2015 | 2a | F-4 | 2.0-3.25 | Will explore parameters of F-4 gun to deliver acceptable microstructure and hardness | HE1100
Chart: Different Plasma guns
| 9MB | F-4 (Phase 2) | 100HE (Phase 2) | 100HE (Phase 2a) | Sinplex Pro (Phase 2a)
 | 1.375 | 1.5 | 2 | 2 | 2.25
 | 0.25 | 1.5 | 0.75 | 0.75 | 0.5

## Slide 45
Injectors Tips Coated and Delivered for Solar Turbines for a Rig Test
Sim

## Slide 46: Summary & Conclusions-I
SPPS YAG TBCs Show Potential For >1500oC Operation Based On Phase Stability, Sinter and CMAS Resistance
This Represents >200oC Advantage Over APS YSZ
Durability of SPPS YAG TBCs ≥ APS YSZ In Thermal Cycle and Erosion Tests
Thermal Conductivity of of SPPS YAG TBCs with IPBs is 0.99 Watt/moK at at room temperature extrapolates to 0.62 at 1300 C based on our earlier results of 1.65 at RT and 0.9 at 1300 C. To Date Doping expected to reduce K by 25% more

## Slide 47: Summary & Conclusions-II
Deposition Efficiency increased from 24% up to 43% using a different Precursor. More improvement sought.
Standoff distance improved from 1.6 inches to 3 inches Further Improvement sought.
Now being applied to Engine parts and separate arrangements for Tech Transfer to a fortune 500 company.

## Slide 48: Summary & Conclusions-II
Engine Manufacturers Show Strong Interest In SPPS YAG TBCs; Are Conducting In-House Testing
Technology Transfer Being Conducted With TBC Coating Suppliers; They Will Conduct Demonstration Trials and Provide Process Economics
SPPS YAG Continues to Show Strong Promise As Higher Temperature (200oC), Sinter-Resistant, CMAS-Resistant, Low K, Low ρ, Durable TBC

## Slide 49: Acknowledgements
Dr. Briggs White, DOE Program Manager, UTSR Program on SPPS YSZ with IPBs
Dr. Patcharin Burke, DOE Program Manager, STTR Phase I, II & IIA Programs on SPPS YAG TBCs
Our Industrial Partners for Phase II SPPS YAG TBCs: Solar Turbines, Siemens Energy, Pratt & Whitney, Praxair and Progressive Surface

## Slide 50
Chart: Thermal Conductivity (W/m-K)
| SPPS YAG without IPBs | SPPS YAG with partial IPBs (Netzsch Sample) | SPPS YAG with IPBs
 | 2.05 | 1.65 | 0.99
Porosity ~23%
HV= 324±60
Porosity ~33%
HV= 260 ±33
Porosity ~15%
HV= 249±175
Thermal Conductivity of different YAG samples

## Slide 51: SPPS YAG TBCs: Praxair Trials
Proprietary and Confidential

## Slide 52
HE-100 Gun Vickers Hardness (Hv): 187±36
YAG
Steel
YAG
SPPS YAG TBCs: Progressive Surface Trials
Proprietary and Confidential

## Slide 53: Summary & Conclusions-II
Engine Manufacturers Continue To Show Strong Interest In SPPS YAG TBCs; Will Conduct In-House Testing
Technology Transfer Being Conducted With TBC Coating Suppliers; They Will Conduct Demonstration Trials and Provide Process Economics
SPPS YAG Continues to Show Strong Promise As Higher Temperature (200oC), Sinter-Resistant, CMAS-Resistant, Low K, Low ρ, Durable TBC
Phase IIA, Starts 4-22-15, Emphasizes Further Conductivity Reduction, Precursor & Processing Improvements, Scale-Up to Complex Geometries
Proprietary and Confidential

## Slide 54: Questions ?

## Slide 55: Laser Flash Apparatus

## Slide 56: Flash Method Schematic

## Slide 57: Flash Method Error
      [4] Taylor RE. Thermal conductivity determinations of thermal barrier coatings. Materials Science and Engineering A245.1998: 160–167

## Slide 58: Spray trials with diluted precursor
15% Dilution, SD: 1.375’’
HV: 374 ± 54
30% Dilution, SD: 1.5’’
HV: 229 ± 25
50% Dilution, SD: 1.5’’
HV: 250 ± 25
25% dilution, SD: 1.375’’
HV: 243 ± 48
DE values show an improvement with higher dilution levels with overall reduction in cost
Repeatable microstructures and hardness were produced with all the precursors
Chart: Dilution of YAG precursor
| 10 | 15 | 25 | 30 | 50
Deposition Efficiency | 23.6 | 26.1 | 25.6 | 26.75 | 32.3
Deposition Rate | 6.23 | 4.95 | 4.96 | 4.65 | 4.46
Chart: Dilution (%)
| 10 | 15 | 20 | 30 | 50
 | 144.53 | 139.92 | 137.94 | 134.65 | 136.91

## Slide 59
SPPS YAG TBCs: Effect of Precursor Concentration
SPPS YAG 5 wt% urea, 1.375”, on SS.
SPPS YAG 5 wt% urea, 10% H2O dilution, 1.375”, on SS.
SPPS YAG 5 wt% urea, 20% H2O dilution, 1.375”, on SS.
Increased Precursor Dilution Produces Denser Harder TBCs

## Slide 60
Addition of Polyvinyl Alcohol (PVA)
YAG, η= 5.9
YAG+1 wt% PVA low MW, η= 7.5
YAG+1 wt% PVA high MW, η= 10.3
Increased precursor viscosity with PVA addition

## Slide 61
Addition of Polyvinyl Alcohol (PVA)
No PVA
Adding PVA increases the microhardness, low MW PVA is more effective (spray distance 1.25”, 1.375”, 1.425”, 1.5”)
Spray distance
Spray distance
Spray distance

## Slide 62
Changing Atomizing Pressure

## Slide 63
SD = 1.375” 1.425” 1.5” 1.625”
Increased Spray Distance at Lower Atomizing Pressure

## Slide 64
HVOF MCrAlY Bond Coat
APS YSZ 13v/o Porosity
APS YSZ Baseline Samples
Haynes 230
Ni-Base Alloy